HENCO brass compression fitting: Sizes 16mm, 18mm, 20mm, 26mm, 32mm.

Fittings shall comply with EN 1254-3 and EN-ISO 21003-2 and be approved by WRAS, DVGW, KIWA, DNV, ATG suitable for the following applications:

- Drinking Water

- Heating

- Underfloor Heating

- Chilled water

- Other applications (on request and after HENCO’s written consent)

The compression fittings shall be manufactured from brass CW617N and have an open clamping ring for multi-layer pipes or a closed clamping ring for EN1057 copper, Carbon steel DIN EN10305 and Stainless steel DIN EN10088/DIN EN10312 pipes as required.   Fitting sealing O-rings shall be made of black EPDM material in accordance with EN681-1 and a synthetic buffer ring to prevent galvanic contact.  The fittings shall be compatible with HENCO multilayer pipes to UNI EN 21003-2. Fittings shall have a maximum working pressure of 16 bar between temperatures of 0°C to +95°C.

Fittings shall be installed and tested following the manufacturer’s installation instructions and according to appropriate codes of practice