**HENCO Full flow manifolds:**  Types VSKEK,

**Fittings shall comply with EN-ISO 21003-2 and be approved by DVGW, KIWA, DNV, ATG suitable for the following applications:**

1. Drinking Water
2. Heating
3. Chilled water
4. Other applications (on request and after HENCO’s written consent)

The modular full flow manifolds shall be manufactured from white PVDF, and come in a 2- or 3-connection version with an alignment feature. Sealing O-rings shall be made of black EPDM material in accordance with EN681-1. Connections to the full flow manifold shall be made using PVDF or brass Eurocone fittings.

The full flow manifolds that uses the Push-Fit connections shall be compatible with Henco multilayer pipes to UNI EN 21003-2. Fittings shall have a maximum working pressure of 16 bar between temperatures of -10°C to +95°C.

The full flow manifold shall be installed and tested following the manufacturer’s installation instructions and according to appropriate codes of practice